## Slide 1: Achieving Optimal RAP Gradation in Processing

## Slide 2: Asphalt Production
From 2020 to 2021, the estimated total amount of asphalt mixture produced in the United States increased from 407.8 million tons to 432.4 million tons, an increase of 6 percent.

## Slide 3: RAP Usage

## Slide 4: RAP: Market and History
The total estimated tons of RAP used in asphalt mixtures was 94.6 million tons in 2021. This represents a 68.9 percent increase from the total estimated tons of RAP used in 2009. Since 2009, total asphalt mixture tonnage has increased only 20.6 percent.
RAP usage during the 2021 construction season is estimated to have reduced the need for 4.7 million tons (26 million barrels) of asphalt binder and more than 89 million tons of aggregate with a total estimated value of more than $3.4 billion.
*Data from NAPA annual Asphalt Pavement Industry Survey

## Slide 5: RAP: Market and History
• The total estimated amount of RAP stockpiled nationwide at the end of the 2021 construction season was about 137 million tons.
• Fractionated RAP represents about 25 percent of RAP use nationwide, and the tons of RAP mixtures produced using softer binders are estimated at 22 percent while tons produced using recycling agents is estimated at 5 percent.
*Data from NAPA annual Asphalt Pavement Industry Survey

## Slide 6: RAP: Market and History
*Data from NAPA annual Asphalt Pavement Industry Survey

## Slide 7: RAP: Market and History
*Data from NAPA annual Asphalt Pavement Industry Survey

## Slide 8: RAP: Fractionating vs Recycling

## Slide 9: RAP: Problems with Single Sizing
Difficult controlling gradation in mixes containing greater than 20% RAP
Stockpiled RAP can segregate and join back together
Tough to get uniform mix

## Slide 10: RAP: Problems with Single Sizing

## Slide 11
¾” (19mm) RAP Bin
RAP: Problems with Single Sizing

## Slide 12
20% RAP Mix:
0.2 x 7.5% AC = 1.5% AC
0.2 x 3.5% AC = 0.7% AC
0.8% Potential AC swing
40% RAP Mix, 1.6% AC Swing
Will this make a difference?
½” x No.4
3.5% AC
No.4 x 0
7.5% AC

## Slide 13: RAP: Obstacles to Fractionating
Reluctance to make changes
Lack of focus
Lack of research
Lack of trained personnel
Unsure of return on investment
Putting out fires

## Slide 14: RAP: Fractionating vs. Recycling
Best use of products given
Crushing and screening
Breaking apart the bond (liberate)
Treating RAP gradation same as virgin mix

## Slide 15
Takes Advantage Of Higher Asphalt Content In “Fine” RAP
Provides Scarce/High Dollar Size Aggregate Material
RAP is worth what it replaces
Allows You To Adjust mix designs
RAP: How Fractionating adds Value

## Slide 17: RAP: Handling
Majority have no special RAP stockpiling
You need RAP stockpiles to be placed on a sloped surface to aid in draining
You need RAP stockpiles to be placed on a paved surface to minimize contamination
RAP stockpiles should be placed under cover to minimize moisture and sunlight exposure

## Slide 18: Mobile & Portable Conveyors
On-site mobility with radial options for easy stockpiling

## Slide 19
Tracked conveyor solutions = 15 Times more capacity
Or at 150 TPH = 2 Days running before you need to reposition
UP TO 70% CHEAPER TO OWN/OPERATE THAN WHEEL LOADER
Track Conveyors

## Slide 20: RAP: Handling
Larger Stockpile Capacity – The telescoping action of the Super Stacker makes it capable of creating stockpiles with 30% more capacity than a standard radial stacker of the same length.

## Slide 21: RAP: Handling

## Slide 22: RAP Processing & Handling

## Slide 23
RAP: Handling

## Slide 24
Take care of your RAP
Keep it clean and uncontaminated
Keep it dry:
Saves drying costs
Fractionates more readily
Can fractionate finer & faster
Use RAP fractions in most profitable ways
RAP: Maximizing Value

## Slide 25: RAP: Processing Options

## Slide 26: RAP: Crushing
Impactor designs meant to break apart the bond that won’t over-crush
Quick adjust aprons and hydraulic variable speed drive to adjust to conditions
Size crushers according to what is needed based on feed product and desired products

## Slide 27: RAP: Horizontal Shaft Impactors
Notes: Generally chosen because of high reduction ratio and capacity
Pioneer currently has three models available:
4233, 42 50 & 5260

## Slide 28
Coarse material requires more amplitude and less frequency
Fine material requires less amplitude and more frequency
Efficient screens will minimize the amount of recirculation in turn meaning more rock stays coated
RAP is sticky and builds up quickly in screenboxes
Understand desired products and also communicate future opportunities
RAP: Screening

## Slide 29: RAP: High Frequency Screens
Coarse material requires more amplitude and Less Frequency
Fine Material requires less amplitude and More Frequency
Utilizes aggressive screen vibration directly to screen media with almost no amplitude applied to side of box
High RPM allows material to stratify and separate at a much faster rate

## Slide 30: High Frequency Screens

## Slide 31: Multi Frequency screens

## Slide 32: RAP: Processing
Look for designs that will help keep components clean
Clean equipment daily
Conveyor designs intended to handle slabby material
Machines that are easy to move
Machines that are easy to run

## Slide 33: RAP: Processing
Millings go directly to the screen first
Ripped material goes to the impactor first

## Slide 34
Ripped material goes in here
Millings go in here
RAP: Processing

## Slide 35: RAP: Processing – Level One
Ideal for fractionating or making one size from millings
Self contained
Easily portable
Low operating cost
Low entry price for processing RAP.

## Slide 36
RAP: Processing – Level One

## Slide 37: RAP: Processing – Level 2
Ideal for fractionating millings
Self contained
On-board HSI crusher
Easily portable
Two or three products
Closed circuit

## Slide 38: RAP: Processing – Level 2

## Slide 39: RAP: Processing – Level 2

## Slide 40: RAP: Processing – Level 3
Will handle any Material size
Multiple configurations
Fractionating
One-size Recycling
Closed Circuit
Open Circuit
High tonnages
Site mobile
Has uses in other materials
Concrete
Aggregate

## Slide 41
RAP: Processing – Level 3

## Slide 42: Stationary System

## Slide 43: RAP: Processing – Level 4
Great for One-Site Operations
Customized to Fit Your Needs
Self Contained or Line Power
Various Tonnage and Feed Size Configurations
On-demand Sizing
Easy Access and Serviceability

## Slide 44: RAP: Processing – Level 4 (Fractionating)
Produce up to five sizes
Portable/Electric
Allows an increase in RAP usage
Offers similar control as virgin product

## Slide 45
RAP: Processing – Level 4 (Fractionating)

## Slide 46
Ripped material goes in here
Millings go in here
RAP: Processing – Level 4 (Fractionating)

## Slide 47: RAP: Processing – Level 4

## Slide 48: Questions