## Slide 1: Enhancing RAP/RAS Mix Performance with BMD: Case Study from Alabama
Suri Gatiganti, Ph.D.
Assistant Research Professor, NCAT

## Slide 2: Background (Benefits of RAS)
Reference: NAPA’s Recycled Material Usage Report
Environmental
Economical
Engineering
Environmental:
Divert Reclaimed Asphalt Singles (RAS) from landfill
In 2022:
  641,000 tons of unprocessed RAS was saved for future use.
  390,000 cubic yards in landfill.
  $37 million in gate fess for disposal
Economical:
Available material and cost savings
In 2022:
  Saved $99 million by using RAS
  134,000 tons (approximately 740,000 barrels) of virgin binder
  336,000 tons of aggregate.
Engineering:
High binder content in RAS materials
Enhance mix properties with angular fine aggregate and fiber
However, there are major performance challenges
Notes: Environmental: In 2022, 641,000 tons of unprocessed RAS was saved for future use. Equivalent to 390,000 cubic yards in landfill and more than $37 million in gate fess for disposal
Economical: In 2022 the Industry saved $99 million by using RAS. Which reduced 134,000 tons (approximately 740,000 barrels) of virgin binder and 336,000 tons of aggregate.

## Slide 3: Background (Challenges)
RAS is a highly oxidized material
  Can weaken the cracking resistance of asphalt mixes
Since 2014, the usage of RAS has been reduced by 65%.
Can we design asphalt mixtures with RAS without compromising performance?
  Taking advantage of Balanced Mix Design (BMD)?
Reference: Williams et al. 2021

## Slide 4: Background (Oklahoma Case Study)
ODOT volumetric mix design does not allow RAS in surface mixes
ODOT BMD specification on surface mixes
  No RAS in surface-course mixtures
Explore the feasibility of designing RAP/RAS surface mixes with balanced performance.

## Slide 5: Background (Oklahoma Case Study)
Reference: NAPA BMD resource guide
Hamburg Wheel Tracking Test (HWTT)
AASHTO T 324
at 50°C
Short-term aged: Loose mix 135oC for 4 hours
10,000 passes to reach 12.5 mm rut depth
Short-term aged: Loose mix 135oC for 4 hours
Indirect Tensile Cracking Test (IDEAL-CT)
ASTM D8225
Conditioning: 2 hours, 25°C in environmental chamber
CTindex ≥ 100
BMD Tests and Criteria

## Slide 6: Background (Oklahoma Case Study)
JMF |  | Virgin BMD | RAP/RAS BMD
Combined Gradation | 1" | 100.0 | 100.0
 | 3/4" | 100.0 | 100.0
 | 1/2" | 96.5 | 96.4
 | 3/8" | 81.6 | 81.2
 | #4 | 56.9 | 55.6
 | #8 | 43.9 | 42.5
 | #16 | 33.9 | 31.2
 | #30 | 25.2 | 22.3
 | #50 | 15.8 | 14.2
 | #100 | 7.9 | 7.6
 | #200 | 3.4 | 3.7
Virgin Binder |  | PG 64-22 | PG 58-28
Additive |  | None | 0.5% LAS
Design Gyration |  | 50 | 50
Asphalt Content, % |  | 5.35 | 5.6
Virgin Asphalt Content, % |  | 5.35 | 4.86
RAP Asphalt Content, % |  | - | 0.35
RAS Asphalt Content, % |  | - | 0.39
RBR, % |  | - | 13.3
Air Voids, % |  | 3.0 | 3.0
VMA, % |  | 14.6 | 15.1
VFA, % |  | 79.7 | 80.3
Dust/asphalt ratio |  | 0.68 | 0.70
Volumetric mix designs failed in BMD
  Virgin (control) mix
  7%RAP, 2%RAS mix
Strategies that worked for RAP/RAS mix
  Lower design air voids (+0.3% binder)
  Softer binder (PG64-22  PG58-28)
  +0.5%LAS
0.5% lower virgin binder

## Slide 7: Background & Objective
ALDOT specification on surface mixes
  Up to 20% RAP
  Up to 20% RAP/RAS (combined), but RAS cannot exceed 3%
    Up to 17% RAP, 3% RAS
Explore the feasibility of designing RAP/RAS surface mixes with higher RAS contents (from 3% to 5%) and balanced performance

## Slide 8: Study Scope
Received two ALDOT-approved volumetric mix designs
  20% RAP mix (control)
  17% RAP, 3% RAS mix
Developed a volumetric mix design with 15% RAP and 5% RAS using the same aggregate stockpiles
Optimized the both mix designs with BMD
  20% RAP mix (control)
  15% RAP, 5% RAS mix

## Slide 9: Volumetric Mix Design Comparison
Mix Design | 20% RAP (Contractor) | 15% RAP, 5% RAS (NCAT)
Virgin Binder | PG 67-22 | PG 67-22
Additive (% total binder) | 0.5 ASA | 0.5 ASA
Total AC (%) | 5.5 | 6.0
Virgin AC (%) | 4.5 | 4.25
RBR (%) | 18.2 | 29.2
Va (%) | 4.0 | 3.5
VMA (%) | 15.5 | 16.0
VFA (%) | 74.2 | 78.2
DP | 1.10 | 1.10
Notes: ASA: Evotherm M1

## Slide 10: ALDOT BMD Specification
BMD for local roads (special provision)
BMD approach: C
  Allows some of the volumetric requirements to be relaxed.
BMD Performance Tests: IDEAL-CT and HT-IDT
  On Short-Term Aged (STA) samples for 2 hours at 275o F
Select Gradation and AC
Conduct Performance Tests
Measure Volumetrics Properties
CTIndex
HT-IDT Strength

## Slide 11: BMD Modification (20% RAP Mix-Control)
Volumetric mix design failed in BMD
Strategies that worked for 20% RAP mix
  Increase 0.3% AC
5.5% AC, PG 67-22
(Volumetric mix design)
5.8% AC, PG 67-22
(BMD Optimized)
Failed rutting test
Passed cracking test
Passed rutting test
Passed cracking test
Failed rutting test
Failed cracking test
Passed rutting test
Failed cracking test

## Slide 12: BMD Modification (RAP/RAS Mix)
Volumetric mix design failed in BMD
  15%RAP & 5%RAS
BMD Modifications Used
  Increase asphalt content
    Did Not work
15% RAP and 5% RAS
(Volumetric mix design)
CTIndex= 28.1
HT-IDT Strength= 36.1 psi

## Slide 13: BMD Modification (RAP/RAS Mix)
Volumetric mix design failed in BMD
  15%RAP & 5%RAS
BMD Modifications Used
  Increase asphalt content
    Did Not work
  Use a softer binder at different asphalt contents
    Worked out
6.0 % AC, PG 52-34
6.5 % AC, PG 52-34
(BMD optimized)
6.0% AC, PG 67-22
(Volumetric mix design)

## Slide 14: BMD Modification (RAP/RAS Mix)
Volumetric mix design failed in BMD
  15%RAP & 5%RAS
BMD Modifications Used
  Increase asphalt content
    Did Not work
  Use a softer binder at different asphalt contents
    Worked out
  Add a recycling agent at different dosages
    Worked out
6.0% AC, PG 67-22, 7.8% RA
(BMD optimized)
6.0% AC, PG 67-22, 6.8% RA
6.0% AC, PG 67-22
(Volumetric mix design)

## Slide 15: BMD Optimization Summary
Two Strategies worked effectively for RAP/RAS mix:
  Used a softer binder and increased AC by 0.5%
  Added a recycling agent (RA)
20% RAP mix
17%RAP & 5%RAS mix
(Recycling agent)
17%RAP & 5%RAS mix
(Softer binder)
Mix Design | 20% RAP | 15% RAP, 5% RAS | 
Virgin Binder | PG 67-22 | PG 52-28/34 | PG 67-22
Additive (% total binder) | 0.5 ASA | 0.5 ASA | 0.5 ASA, 5.5 RA
Total AC (%) | 5.8 | 6.5 | 6.0
Virgin AC (%) | 4.8 | 4.8 | 4.3
RBR (%) | 17.2 | 26.9 | 29.2
Va (%) | 3.2 | 2.3 | 3.5
VMA (%) | 16.3 | 16.7 | 16.0
VFA (%) | 80.4 | 85.8 | 78.2
DP | 1.0 | 1.0 | 1.1

## Slide 16: Summary and Conclusions
It is feasible to design RAP/RAS mixes with satisfactory performance using BMD
  With 15%RAP, 5% RAS compared to 20%RAP mix
Strategies that best worked in this study
  Use a softer binder and increased AC by 0.5%
  Add a recycling agent
Other strategies such as change in gradation, use of other recycling agents, etc. can be used
  To design RAS mixes with satisfactory performance and better economics

## Slide 17
Dr. Suri Gatiganti
Assistant Research Professor
National Center for Asphalt Technology
szg0094@auburn.edu